ЕВРОПЕЙСКИ СОЦИАЛЕН ФОНД 2007 – 2013

ОПЕРАТИВНА ПРОГРАМА

„РАЗВИТИЕ НА ЧОВЕШКИТЕ РЕСУРСИ”

ПРОЕКТ BG051PO001-3.3.06-0014: “ЦЕНТЪР ПО МАТЕМАТИЧНО МОДЕЛИРАНЕ И КОМПЮТЪРНА СИМУЛАЦИЯ ЗА ПОДГОТОВКА И РАЗВИТИЕ НА МЛАДИ ИЗСЛЕДОВАТЕЛИ ”

Проектът се осъществява с финансовата подкрепа на Оперативна програма „Развитие на човешките ресурси”, съфинансирана от Европейския социален фонд на Европейския съюз

## “SIXTH BALKAN CONFERENCE ON GLASS SCIENCE AND TECHNOLOGY”

## “18th CONFERENCE ON GLASS AND CERAMICS”

from 01th to 04th October 2014, Nesebar, Bulgaria

. SYNTHESIS AND CHARACTERIZATION OF SILICA HYBRID MATERIALS APPLICABLE FOR DEFECT REMEDIATION OF CONCRETE

G. Chernev, E. Todorova, G. Chernev, St. Djambazov

University of Chemical Technology and Metallurgy, 8 Kl. Ohridski blvd., 1756, Sofia, Bulgaria

Abstract

Silica hybrid materials applicable for defect remediation of concrete, based on silica network with participation of organic components – chitosan and polyethylene glycol and bacteria calls were successfully obtained via sol-gel synthesis. Tetraethyl orthosilicate precursor was used as silica network former. The organic components were used for improving the plasticity and reactivity of the silica network, as well as activity of the immobilized bacteria cells. Structural analyses were used for establishment of the organic component influence on the hybrid structure and immobilized bacteria cells vitality. The results showed that silica hybrid materials with amorphous, homogeneous structures into which the organic components are evenly distributed were obtained. Synthesized novel hybrid materials were applied as coating on concrete samples with cracks for establishment of the self healing properties.

This paper has been produced with the financial assistance of the European Social Fund, project number BG051PO001-3.3.06-0014. The author is responsible for the content of this material, and under no circumstances can be considered as an official position of the European Union and the Ministry of Education and Science of Bulgaria